# Comprehensive IPQC Testing Procedures for Solar Panel Manufacturing

## Introduction

This document provides detailed testing procedures, acceptance criteria, and value interpretations for the In-Process Quality Control (IPQC) check sheet used in solar photovoltaic module manufacturing at Gautam Solar Private Limited. Each test is explained in detail including methodology, equipment required, and how to interpret and record results.

## STAGE 1: SHOP FLOOR ENVIRONMENT MONITORING

### 1.1 Temperature Monitoring

Test Frequency: Once per shift
Equipment Required: Calibrated digital thermometer or environmental monitoring system
Test Procedure:

- Place the thermometer in the central area of the production floor

- Allow temperature reading to stabilize (minimum 5 minutes)

- Record the temperature in degrees Celsius

- Ensure reading is taken away from direct heat sources or air conditioning vents

Acceptance Criteria: 25±2°C (23°C to 27°C)
Value to Record: Actual temperature in °C
Importance: Temperature affects EVA curing, adhesive properties, and soldering quality. Temperatures outside the acceptable range can lead to:

- Below 23°C: Poor EVA flow during lamination, inadequate curing, weak adhesion between glass and cells

- Above 27°C: Accelerated curing of adhesives before proper positioning, thermal stress on cells, increased risk of microcracks

Troubleshooting:

- If temperature is outside range, adjust HVAC systems

- Check for localized heat sources affecting readings

- Verify thermometer calibration monthly against a standard

### 1.2 Humidity Monitoring

Test Frequency: Once per shift
Equipment Required: Calibrated hygrometer or environmental monitoring system
Test Procedure:

- Place the hygrometer in the central area of the production floor

- Allow humidity reading to stabilize (minimum 5 minutes)

- Record the relative humidity percentage

- Ensure reading is taken away from moisture sources and water stations

Acceptance Criteria: RH ≤60%
Value to Record: Actual relative humidity percentage
Importance: Humidity affects:

- Solderability of cells and interconnects

- Adhesive curing and bonding strength

- Potential moisture ingress into modules

- High humidity (>60%) can cause:

  - Poor soldering joints

  - Moisture trapped in modules during lamination

  - Increased risk of potential induced degradation (PID) during module lifetime

  - Delamination risk increases

Troubleshooting:

- If humidity exceeds 60%, check dehumidification systems

- Inspect for water leaks or other moisture sources in production area

- Consider adding additional dehumidifiers in critical process areas

## STAGE 2: GLASS LOADER

### 2.1 Glass Dimension (L×W×T)

Test Frequency: Once per shift
Equipment Required: Calibrated digital caliper, measuring tape or laser distance meter
Test Procedure:

- Select one glass sheet from the current production batch

- Measure length (L) along both edges and record average

- Measure width (W) along both edges and record average

- Measure thickness (T) at all four corners and center, record average

- Clean measuring equipment between measurements

Acceptance Criteria:

- Length: 2272 ± 1.5 mm (2270.5 mm to 2273.5 mm)

- Width: 1128 ± 1.5 mm (1126.5 mm to 1129.5 mm)

- Thickness: 2 ± 0.2 mm (1.8 mm to 2.2 mm)

Value to Record: Actual measurements in mm for L, W, and T
Importance: Glass dimensions directly impact:

- Fit in framing equipment

- Cell arrangement and string placement

- Overall module dimensions and mounting compatibility

- Out-of-spec glass can cause:

  - Misalignment in automated equipment

  - Mechanical stress on cells during framing

  - Risk of glass breakage during production or in the field

Troubleshooting:

- If dimensions are out of spec, isolate the affected batch

- Check with glass supplier for dimensional issues

- Adjust handling equipment if necessary

- Monitor for patterns in measurement deviations

### 2.2 Glass Appearance (Visual)

Test Frequency: Once per shift
Equipment Required: Inspection light box or bright white light source, magnifying glass (optional)
Test Procedure:

- Select one glass sheet from current production batch

- Place glass on clean, white background or light table

- Inspect entire surface in good lighting conditions, looking for:

  - Cracks (any visible break in glass)

  - Chips (small breakage at edges)

  - Scratches (surface damage that catches fingernail)

  - Line marks (visible linear patterns)

  - Bubbles (internal air inclusions)

  - Inclusions (foreign material in glass)

- Check all edges and corners for damage

- Record any defects found by type, size, and location

Acceptance Criteria: No glass breakage, cracks, scratches, or line marks allowed
Value to Record: "Pass" or specific defects found
Importance: Glass quality impacts:

- Mechanical strength of finished module

- Light transmission to cells

- Risk of glass breakage during subsequent processes

- Aesthetic quality of finished product

- Defects can:

  - Lead to glass failure under thermal stress

  - Create pressure points on cells during lamination

  - Reduce module efficiency

  - Create visual irregularities

Troubleshooting:

- If defects are found, trace glass batch and inspect more samples

- Check glass handling equipment for damage points

- Ensure proper glass storage and handling procedures

- Provide feedback to glass supplier if defects are recurring

## STAGE 3: EVA/EPE CUTTING

### 3.1 EVA/EPE Type

Test Frequency: Once per shift
Equipment Required: Bill of Materials (BOM), magnifying glass, UV light for special EVA types
Test Procedure:

- Check EVA/EPE packaging or label for material specification

- Verify against approved BOM and project specifications

- Check for manufacturer markings or identifiers

- For EVA, check if it's fast cure or standard cure type as specified

- Verify anti-PID properties if specified

- Record material type, manufacturer, and batch number

Acceptance Criteria: Material must match approved BOM specification
Value to Record: Actual material type, manufacturer, batch number
Importance: EVA/EPE material properties impact:

- Lamination cycle requirements

- Module durability and aging characteristics

- Protection against potential induced degradation (PID)

- Incorrect material can cause:

  - Improper adhesion between glass and cells

  - Yellowing or degradation in field conditions

  - Inappropriate curing during lamination

  - Cell corrosion or degradation

Troubleshooting:

- If incorrect material is identified, immediately set aside and notify supervisor

- Check for mixed materials in storage area

- Verify BOM updates have been communicated to production

- Confirm material meets IEC certification requirements

### 3.2 EVA/EPE Dimension (L×W×T)

Test Frequency: Once per shift
Equipment Required: Calibrated digital caliper, clean cutting surface, measuring tape
Test Procedure:

- Select one cut EVA/EPE sheet from current production

- Place on clean, flat surface

- Measure length (L) at three points (both ends and middle)

- Measure width (W) at three points (both ends and middle)

- Measure thickness (T) at each corner and center

- Calculate and record averages

Acceptance Criteria: Must match glass dimensions:

- Length: 2272 ± 1.5 mm

- Width: 1128 ± 1.5 mm

- Thickness: Per specification (typically 0.45-0.5 mm per layer)

Value to Record: Actual measurements in mm for L, W, and T
Importance: EVA/EPE dimensions affect:

- Complete coverage of cell area

- Proper edge sealing

- Even distribution during lamination

- Undersized EVA can lead to:

  - Exposed cell areas

  - Edge delamination

  - Moisture ingress paths

- Oversized EVA can cause:

  - Excess material flow during lamination

  - Contamination of vacuum channels

  - Uneven lamination

Troubleshooting:

- If dimensions are incorrect, check cutting equipment settings

- Verify sheet position during cutting operation

- Check for material stretching during handling

- Inspect cutting blades for wear

### 3.3 EVA/EPE Status

Test Frequency: Once per shift
Equipment Required: Inspection light table, lint-free gloves, magnifying glass
Test Procedure:

- Select one cut EVA/EPE sheet from current production

- Place on clean, white background or light table

- Inspect entire surface for:

  - Foreign particles (dust, fibers, debris)

  - Cuts or tears

  - Non-uniform embossing pattern

  - Wrinkles or folds

  - Air bubbles between layers

- Check manufacturing date on packaging

- Record any defects found by type, size and location

Acceptance Criteria: No dust, foreign particles, cuts, or non-uniform embossing allowed. Manufacturing date must be within shelf life period.
Value to Record: "Pass" or specific defects found
Importance: EVA/EPE quality directly impacts:

- Lamination quality and visual appearance

- Cell protection and encapsulation

- Long-term reliability

- Defects can cause:

  - Voids or bubbles in laminated module

  - Poor adhesion areas

  - Reduced module lifetime

  - Potential hot spots due to poor thermal conductivity

Troubleshooting:

- If defects are found, check handling and storage conditions

- Verify clean room protocols are being followed

- Inspect cutting equipment for contaminants

- Check expiry date and storage conditions of EVA/EPE

## STAGE 4: CELL CUTTING MACHINE & CELL LOADING

### 4.1 Cell Manufacturer & Efficiency

Test Frequency: Once per shift
Equipment Required: Documentation (GSPL/IPQC/QA/001), magnifying glass, cell packaging/labels
Test Procedure:

- Check cell packaging or label for manufacturer information

- Verify cell efficiency rating from manufacturer documentation

- Cross-check against project specifications and BOM

- Record manufacturer name and efficiency rating

- Verify batches are not mixed if different manufacturers are used

Acceptance Criteria: Must match specification per document GSPL/IPQC/QA/001
Value to Record: Actual manufacturer name and efficiency percentage
Importance: Cell manufacturer and efficiency affect:

- Module power output and binning

- Consistency of manufacturing process

- Material compatibility (especially for soldering)

- Using incorrect cells can result in:

  - Lower module power than rated

  - Inconsistent electrical characteristics

  - Warranty issues

  - Color mismatch between cells

Troubleshooting:

- If mismatch is found, verify if there was an approved change request

- Check if cells were properly segregated in storage

- Verify if cells are within the same power bin

- Check for counterfeit products if appearance differs from standard

### 4.2 Cell Size (L×W)

Test Frequency: Once per shift
Equipment Required: Calibrated digital caliper, ESD-safe handling tools, document GSPL/IPQC/QC/006
Test Procedure:

- Using ESD protection, select sample cells from current production

- Place on clean, flat surface

- Measure length (L) and width (W) at center of each edge

- Record measurements

- Compare to specifications in document GSPL/IPQC/QC/006

Acceptance Criteria: Must match dimensions in document GSPL/IPQC/QC/006 (typically for mono PERC cells: 166×166mm, 182×182mm, or 210×210mm depending on technology)
Value to Record: Actual measurements in mm
Importance: Cell dimensions affect:

- String layout and spacing

- Interconnection positions

- Overall module power (larger cells generally mean higher power)

- Incorrect dimensions can cause:

  - String misalignment

  - Improper tabbing wire placement

  - Ribbon stress during thermal cycling

Troubleshooting:

- If dimensions are incorrect, verify if there was a cell type change

- Check if cells were mixed during storage

- Ensure specification documents are updated

### 4.3 Cell Condition

Test Frequency: Once per shift
Equipment Required: Document GSPL/IPQC/QC/009, inspection light table, magnifying glass
Test Procedure:

- Using ESD protection, select sample cells from current production

- Place on clean, well-lit inspection surface

- Inspect each cell for:

  - Microcracks (may require backlight)

  - Chipped edges

  - Bus bar quality and straightness

  - Color consistency

  - Finger interruptions

  - Surface contamination

  - Anti-reflection coating uniformity

- Record any defects according to categories in document GSPL/IPQC/QC/009

Acceptance Criteria: Must meet inspection standards per document GSPL/IPQC/QC/009
Value to Record: "Pass" or specific defects found
Importance: Cell condition affects:

- Module electrical performance

- Long-term reliability

- Solderability during stringing

- Defects can cause:

  - Power loss

  - Hot spots

  - Cell fractures during lamination

  - Increased series resistance

Troubleshooting:

- If defects exceed acceptance limits, isolate the batch

- Check cell handling equipment for damage points

- Review handling procedures with operators

- Capture images of defects for supplier feedback

### 4.4 Cleanliness of Cell Loading Area

Test Frequency: Once per shift
Equipment Required: Inspection light, lint-free wipes
Test Procedure:

- Perform visual inspection of entire cell loading area

- Check for:

  - Dust particles

  - Cell fragments

  - Tabbing wire scraps

  - Flux residue

  - Other foreign materials

- Inspect vacuum cups and transfer mechanisms

- Verify cleaning schedule has been followed

- Record observations and cleanliness status

Acceptance Criteria: No unwanted or waste material should be at cell loading area
Value to Record: "Clean" or specific contamination found
Importance: Cleanliness impacts:

- Cell damage during handling

- Foreign particle inclusion in module

- Quality of cell placement

- Contamination can cause:

  - Cell microcracks from particles

  - Soldering defects from contamination

  - Visual defects in finished modules

  - Reduced yield

Troubleshooting:

- If area is contaminated, stop production and clean thoroughly

- Check cleaning schedule and procedures

- Verify air filtration systems are functioning

- Inspect operator PPE for potential contamination sources

## STAGE 5: TABBER & STRINGER

### 5.1 Verification of Process Parameter

Test Frequency: Once per shift
Equipment Required: Process card/documentation, stringer HMI (Human Machine Interface)
Test Procedure:

- Access the stringer machine control system

- Record the following parameters:

  - Soldering temperature (typically 260-320°C)

  - Conveyor speed

  - Flux application rate

  - Pressure settings for soldering heads

  - Preheat temperature

  - Tabbing ribbon width and thickness

- Compare with process card specifications

- Verify any recent parameter adjustments are approved and documented

Acceptance Criteria: All parameters must match process card specifications
Value to Record: Actual parameter values compared to specifications
Importance: Process parameters affect:

- Soldering quality and strength

- Cell stress during tabbing process

- Ribbon alignment

- Incorrect settings can cause:

  - Cold or overheated solder joints

  - Cell cracking during soldering

  - Ribbon misalignment

  - Flux residue issues

Troubleshooting:

- If parameters deviate, reset to specification values

- Check for unauthorized changes to settings

- Verify if process card is the latest revision

- After adjustment, produce test string and verify quality

### 5.2 Cell Cross Cutting

Test Frequency: Once per stringer per shift
Equipment Required: Measuring caliper, sample cell/string
Test Procedure:

- Select sample half-cell from production

- Measure cut edge on both sides

- Verify cut is centered on cell

- Check for edge chipping or irregular cutting

- Measure cutting width precision

- Record measurements and observations

Acceptance Criteria: Both side cutting should be equal (tolerance typically ±0.5mm)
Value to Record: Actual measurements of both sides
Importance: Symmetrical cutting ensures:

- Proper cell electrical characteristics

- Consistent string length

- Proper fit in module layout

- Asymmetrical cutting can cause:

  - Varied electrical properties between cells

  - Misalignment in string layout

  - Stress concentration points

Troubleshooting:

- If uneven cutting is found, check cutting blade alignment

- Verify cell positioning before cutting

- Check blade wear and replace if necessary

- Recalibrate cutting mechanism if needed

### 5.3 String Length

Test Frequency: 1 string per stringer per shift
Equipment Required: Document GSPL/PLV/003, measuring tape or dedicated fixture
Test Procedure:

- Select completed string from production

- Place on flat measurement surface

- Measure total length of interconnected cells

- Verify measurement meets specification in document GSPL/PLV/003

- Check for uniform spacing between cells

- Record string length and spacing observations

Acceptance Criteria: Must meet specification per document GSPL/PLV/003
Value to Record: Actual measured length in mm
Importance: String length affects:

- Fit in module layout

- Electrical interconnection alignment

- Gap consistency

- Incorrect string length can cause:

  - Stress on interconnects during temperature changes

  - Difficulty in string placement

  - Improper busbar alignment

Troubleshooting:

- If length is out of specification, check cell spacing settings

- Verify ribbon tension in stringer

- Check for cell displacement during handling

- Adjust string spacing parameters if necessary

### 5.4 Cell to Cell Gap

Test Frequency: 1 string per TS (tabber stringer) per shift
Equipment Required: Document GSPL/ELV/003, digital caliper or optical measurement system
Test Procedure:

- Select completed string from production

- Measure gaps between each adjacent cell in the string

- Record individual measurements

- Calculate average gap distance

- Verify against specifications in document GSPL/ELV/003

Acceptance Criteria: Must meet specification per document GSPL/ELV/003 (typically 2.0±0.5mm)
Value to Record: Individual and average gap measurements in mm
Importance: Cell spacing affects:

- String flexibility during lamination

- Stress distribution during thermal cycling

- Overall string length

- Irregular spacing can cause:

  - Ribbon stress points

  - Uneven visual appearance

  - Cell cracking during temperature changes

Troubleshooting:

- If gaps are inconsistent, check stringer transport mechanism

- Verify solder pad positions are consistent

- Check ribbon feed tension

- Inspect for mechanical obstructions in cell transport

### 5.5 Verification of Soldering

Test Frequency: Once per shift
Equipment Required: Process card, magnifying glass, inspection light
Test Procedure:

- Select completed string from production

- Visually inspect each solder point for:

  - Complete coverage of solder pad

  - Proper wetting of solder

  - No excess solder spillage

  - No burns or discoloration around solder points

  - Ribbon alignment on bus bars

- Verify soldering matches process card requirements

- Document any defects observed

Acceptance Criteria: Must meet specifications in process card
Value to Record: "Pass" or specific defects found
Importance: Soldering quality affects:

- Electrical connection reliability

- Series resistance of module

- Long-term durability

- Poor soldering can cause:

  - Increased series resistance

  - Hot spots in operation

  - Connection failures under thermal cycling

  - Power degradation over time

Troubleshooting:

- If defects are found, check soldering temperature and pressure

- Verify ribbon surface cleanliness

- Check flux application rate and coverage

- Inspect soldering heads for contamination or wear

### 5.6 Peel Strength

Test Frequency: 2 cells each stringer (front & back) per shift
Equipment Required: Calibrated peel strength tester, sample cells/strings
Test Procedure:

- Select sample cells with soldered ribbons

- Attach ribbon end to peel strength tester clamp

- Set 90° peel angle

- Initiate test and record peak force required to separate ribbon

- Test both front and back side connections

- Record peel strength values

Acceptance Criteria: ≥1N peel strength
Value to Record: Actual measured force in Newtons
Importance: Peel strength indicates:

- Mechanical durability of connections

- Quality of soldering process

- Resistance to thermal stress

- Low peel strength can lead to:

  - Ribbon detachment during handling

  - Failed connections during temperature cycling

  - Increasing series resistance over time

  - Module power degradation

Troubleshooting:

- If below specification, check soldering parameters

- Verify ribbon and bus bar surface cleanliness

- Check flux type and application

- Review ribbon material properties and compatibility

### 5.7 Visual Check after Stringing

Test Frequency: Once per shift
Equipment Required: Document GSPL/IPQC/QA/001, inspection light table
Test Procedure:

- Place completed string on inspection surface

- Check for:

  - Cell cracks or damage

  - Ribbon alignment on busbars

  - Excess flux residue

  - Cell chipping from handling

  - Ribbon kinks or damage

- Verify visual quality meets standards in document GSPL/IPQC/QA/001

- Record observations and defects

Acceptance Criteria: Must meet standards per document GSPL/IPQC/QA/001
Value to Record: "Pass" or specific defects found
Importance: Visual quality ensures:

- Physical integrity before subsequent processes

- Identification of handling damage

- Detection of process issues

- Defects can indicate:

  - Equipment misalignment

  - Operator handling issues

  - Machine maintenance needs

  - Material property changes

Troubleshooting:

- If defects are found, identify patterns by location

- Check for specific machine stations causing damage

- Review handling procedures

- Increase sampling frequency to isolate cause

### 5.8 EL Image of Strings

Test Frequency: 1 string per TS (tabber stringer) per shift
Equipment Required: Document GSPL/ELV/003, EL imaging system, darkroom or light-sealed test area
Test Procedure:

- Place completed string in EL imaging station

- Connect to power supply with appropriate current (typically 8-10A for a string)

- Capture EL image in darkened environment

- Analyze image for:

  - Microcracks (appearing as dark lines)

  - Inactive areas (appear dark)

  - Soldering defects (non-uniform brightness along busbars)

  - Cell defects (dark spots, finger interruptions)

- Compare against acceptance criteria in document GSPL/ELV/003

Acceptance Criteria: Must meet standards per document GSPL/ELV/003
Value to Record: "Pass" or specific defects found with positions
Importance: EL imaging reveals:

- Cell damage invisible to naked eye

- Quality of electrical connections

- Cell activation uniformity

- Defects can cause:

  - Power loss

  - Reliability issues

  - Hot spots during operation

  - Progressive degradation

Troubleshooting:

- If defects are found, categorize by type and location

- Check machine settings associated with specific defect types

- Review handling procedures if cracks are common

- Correlate with previous visual inspection results

## STAGE 6: AUTO STRING LAYUP

### 6.1 String to String Gap

Test Frequency: Once per shift
Equipment Required: Process card, module drawing, precision ruler or caliper
Test Procedure:

- After string layup, measure the gap between adjacent strings

- Take measurements at three points (top, middle, bottom)

- Record all measurements

- Calculate average gap

- Compare to specification in process card and module drawing

Acceptance Criteria: Must match process card and module drawing specifications (typically 2-4mm depending on module design)
Value to Record: Actual measured gap in mm
Importance: String spacing affects:

- Module electrical configuration

- Appearance uniformity

- Light reflection and absorption

- Improper spacing can cause:

  - Risk of string contact under thermal expansion

  - Uneven visual appearance

  - Reduced module efficiency due to inactive area

Troubleshooting:

- If gaps are inconsistent, check string layup equipment alignment

- Verify program settings for the specific module model

- Check for mechanical obstructions in layup process

- Ensure correct module design is selected in machine program

### 6.2 Cell Edge to Glass Edge Distance

Test Frequency: Once per shift
Equipment Required: Module drawing, precision ruler or caliper
Test Procedure:

- After string layup, measure distance from outermost cell edges to corresponding glass edges:

  - Top (distance from top cells to top glass edge)

  - Bottom (distance from bottom cells to bottom glass edge)

  - Left side (distance from leftmost cells to left glass edge)

  - Right side (distance from rightmost cells to right glass edge)

- Record all four measurements

- Compare to specifications in module drawing

Acceptance Criteria: Must meet specifications in process card/drawing for:

- Top edge distance

- Bottom edge distance

- Side edge distances
(Typically 20-30mm depending on module design)

Value to Record: Actual measurements in mm for all four edges
Importance: Edge distances affect:

- Frame compatibility

- Edge seal integrity

- Junction box placement

- Weather sealing effectiveness

- Insufficient edge distance can cause:

  - Risk of cell contact with frame

  - Inadequate edge sealing

  - Potential moisture ingress paths

  - Mechanical stress during framing

Troubleshooting:

- If distances are incorrect, check glass positioning in layup station

- Verify centering mechanism functionality

- Check for program updates for different module designs

- Ensure correct string lengths were used

### 6.3 Soldering Peel Strength between Ribbon to Busbar Interconnector

Test Frequency: Once per shift
Equipment Required: Calibrated peel strength tester, sample interconnection
Test Procedure:

- Select sample with busbar to ribbon interconnection

- Secure module side of joint

- Attach peel tester to ribbon

- Set 90° peel angle

- Initiate test and record force required to separate connection

- Perform multiple tests on different interconnection points

- Calculate average peel strength

Acceptance Criteria: ≥2N
Value to Record: Actual measured force in Newtons
Importance: Interconnection strength affects:

- Power transfer efficiency

- Long-term reliability

- Thermal cycling durability

- Weak connections can cause:

  - Increased series resistance

  - Power loss over time

  - Open circuits under thermal stress

  - Hot spots during operation

Troubleshooting:

- If below specification, check interconnect soldering parameters

- Verify ribbon and busbar surface cleanliness

- Check ribbon and busbar material compatibility

- Review soldering iron temperature and duration

### 6.4 Terminal Busbar to Edge of Cell

Test Frequency: Once per shift
Equipment Required: Document GSPL/TS/008, precision caliper or digital microscope
Test Procedure:

- Select sample with terminal busbar connections

- Measure distance from terminal busbar edge to cell edge

- Take measurements at multiple points along busbar

- Record all measurements and calculate average

- Compare to specifications in document GSPL/TS/008

Acceptance Criteria: Must meet specifications per document GSPL/TS/008
Value to Record: Actual measured distance in mm
Importance: Busbar positioning affects:

- Electrical path efficiency

- Thermal stress distribution

- Risk of short circuits

- Improper positioning can cause:

  - Increased resistance

  - Risk of edge short circuits

  - Uneven current distribution

  - Thermal stress points

Troubleshooting:

- If misaligned, check busbar placement equipment

- Verify busbar cutting precision

- Check alignment guides in layup equipment

- Review operator training for manual processes

### 6.5 Soldering Quality of Ribbon to Busbar

Test Frequency: Every 4 hours per shift
Equipment Required: Magnifying glass, inspection light
Test Procedure:

- Visually inspect multiple ribbon to busbar soldering points

- Check for:

  - Complete solder coverage

  - No dry joints (appearing dull or grainy)

  - No excess solder (causing bumps or bridging)

  - No burning or discoloration

  - No missed connections

- Record observations for each inspection point

Acceptance Criteria: No dry/poor soldering allowed
Value to Record: "Pass" or specific defects found
Importance: Soldering quality affects:

- Electrical connection reliability

- Series resistance of module

- Heat dissipation at connection points

- Poor soldering can cause:

  - Connection failure under thermal cycling

  - Increased resistance and power loss

  - Hot spots

  - Accelerated degradation

Troubleshooting:

- If defects found, check soldering temperature

- Verify contact time and pressure

- Check for oxide formation on materials

- Review flux type and application method

### 6.6 Top & Bottom Creepage Distance/Terminal Busbar to Glass Edge

Test Frequency: Every 4 hours per shift
Equipment Required: Process card/drawing, precision ruler or caliper
Test Procedure:

- Measure distance from terminal busbar to corresponding glass edge

- Take measurements at multiple points along busbar edge

- Record minimum distance for each busbar

- Compare to specifications in process card/drawing

Acceptance Criteria: Creepage distance should be as per process card/drawing (typically minimum 12.7mm for 1000V systems or 25mm for 1500V systems)
Value to Record: Actual measured minimum distance in mm
Importance: Creepage distance affects:

- Electrical safety and isolation

- High voltage leakage prevention

- Certification compliance

- Insufficient distance can cause:

  - Safety certification failure

  - Potential leakage current paths

  - Electrical arcing risk under wet conditions

  - Reduced system voltage rating

Troubleshooting:

- If below specification, check busbar positioning system

- Verify glass dimension and tolerance

- Check cell layout positioning

- Review process card for correct specification

## STAGE 7: AUTO BUSSING & TAPPING

### 7.1 Verification of Process Parameter

Test Frequency: Once per shift Equipment Required: Machine specification document, auto bussing/tapping machine HMI Test Procedure:

- Access machine control system

- Record the following parameters:

  - Temperature settings for soldering (typically 320-380°C)

  - Adhesive tape tension

  - Pressure settings

  - Cycle time

  - Feed rates

- Compare with machine specification document

- Verify parameters match current product requirements

Acceptance Criteria: As per machine specification Value to Record: Actual parameters vs. specification requirements

Importance: Proper parameters ensure:

- Correct tape application

- Proper soldering of busbars

- Consistent process timing

Improper settings can cause:

- Loose tape application

- Poor busbar soldering

- Misaligned components

- Process inconsistencies

Troubleshooting:

- If parameters deviate, reset to specification values

- Check for unauthorized changes

- Verify machine calibration status

- Perform test cycle after adjustment

### 7.2 Quality of Auto Taping

Test Frequency: Every 4 hours per shift Equipment Required: Visual inspection equipment, sample module Test Procedure:

- Visually inspect tape application across module

- Check for:

  - Proper positioning over strings

  - Uniform adhesion with no bubbles

  - No wrinkles or folds

  - Cell alignment maintained

Acceptance Criteria: Taping should be proper, no cell shifting allowed Value to Record: "Pass" or specific defects found

Importance: Proper taping ensures:

- Cell alignment and stability

- Protection during subsequent processes

- Proper electrical isolation

Improper taping can cause:

- Cell movement during handling

- Inconsistent electrical connections

- Potential short circuits

- Visual defects in final module

Troubleshooting:

- Check tape tension settings

- Verify tape quality and adhesive properties

- Inspect application rollers for debris or damage

- Check for environmental factors affecting adhesion

### 7.3 Position Verification of RFID & Logo Patch on Module

Test Frequency: Every 4 hours per shift Equipment Required: Visual inspection, measuring tools Test Procedure:

- Inspect position of RFID tag and logo patch

- Verify alignment with reference markers

- Check for secure attachment

- Ensure no tilt or misalignment

Acceptance Criteria: Should not be tilted Value to Record: Position status and any deviations

Importance: Proper positioning ensures:

- Accurate module identification

- Professional appearance

- Consistent branding

- Reliable RFID scanning

Improper positioning can cause:

- Difficulty in scanning/tracking modules

- Unprofessional appearance

- Customer rejection based on cosmetics

- Inconsistent brand representation

Troubleshooting:

- Check application equipment alignment

- Verify reference markers are correct

- Inspect adhesive quality

- Train operators on proper placement techniques

## STAGE 8: EVA

### 8.1 EVA/EPE Type

Test Frequency: Once per shift Equipment Required: Bill of Materials (BOM), magnifying glass, UV light for special EVA types Test Procedure:

- Check EVA/EPE packaging or label for material specification

- Verify against approved BOM and project specifications

- Check for manufacturer markings or identifiers

- For EVA, check if it's fast cure or standard cure type as specified

- Verify anti-PID properties if specified

- Record material type, manufacturer, and batch number

Acceptance Criteria: Material must match approved BOM specification (As per Specification) Value to Record: Actual material type, manufacturer, batch number

Importance: EVA/EPE material properties impact:

- Lamination cycle requirements

- Module durability and aging characteristics

- Protection against potential induced degradation (PID)

Incorrect material can cause:

- Improper adhesion between glass and cells

- Yellowing or degradation in field conditions

- Inappropriate curing during lamination

- Cell corrosion or degradation

Troubleshooting:

- If incorrect material is identified, immediately set aside and notify supervisor

- Check for mixed materials in storage area

- Verify BOM updates have been communicated to production

- Confirm material meets IEC certification requirements

### 8.2 EVA/EPE Dimension (L×W×T)

Test Frequency: Once per shift Equipment Required: Calibrated digital caliper, clean cutting surface, measuring tape Test Procedure:

- Select one cut EVA/EPE sheet from current production

- Place on clean, flat surface

- Measure length (L) at three points (both ends and middle)

- Measure width (W) at three points (both ends and middle)

- Measure thickness (T) at each corner and center

- Calculate and record averages

Acceptance Criteria: 2272(±1.5)mm × 1128(±1.5)mm × 2.0(±0.20)mm Value to Record: Actual measurements in mm for L, W, and T

Importance: EVA/EPE dimensions affect:

- Complete coverage of cell area

- Proper edge sealing

- Even distribution during lamination

Incorrect dimensions can cause:

- Exposed cell areas if undersized

- Edge delamination

- Moisture ingress paths

- Excess material flow during lamination if oversized

- Contamination of vacuum channels

- Uneven lamination

Troubleshooting:

- If dimensions are incorrect, check cutting equipment settings

- Verify sheet position during cutting operation

- Check for material stretching during handling

- Inspect cutting blades for wear

### 8.3 EVA/EPE Status

Test Frequency: Once per shift Equipment Required: Inspection light table, lint-free gloves, magnifying glass Test Procedure:

- Select one cut EVA/EPE sheet from current production

- Place on clean, white background or light table

- Inspect entire surface for:

  - Foreign particles (dust, fibers, debris)

  - Cuts or tears

  - Non-uniform embossing pattern

  - Wrinkles or folds

  - Air bubbles between layers

- Check manufacturing date on packaging

- Record any defects found by type, size and location

Acceptance Criteria: Not allowed dust & foreign particle/Cut & non-Uniform Embossing /Mfg Date Value to Record: "Pass" or specific defects found

Importance: EVA/EPE quality directly impacts:

- Lamination quality and visual appearance

- Cell protection and encapsulation

- Long-term reliability

Defects can cause:

- Voids or bubbles in laminated module

- Poor adhesion areas

- Reduced module lifetime

- Potential hot spots due to poor thermal conductivity

Troubleshooting:

- If defects are found, check handling and storage conditions

- Verify clean room protocols are being followed

- Inspect cutting equipment for contaminants

- Check expiry date and storage conditions of EVA/EPE

## STAGE 9: BACK GLASS LOADER

### 9.1 Glass Dimension (L×W×T)

Test Frequency: Once per shift Equipment Required: Calibrated digital caliper, measuring tape or laser distance meter Test Procedure:

- Select one glass sheet from the current production batch

- Measure length (L) along both edges and record average

- Measure width (W) along both edges and record average

- Measure thickness (T) at all four corners and center, record average

- Clean measuring equipment between measurements

Acceptance Criteria: 2272(±1.5)mm × 1128(±1.5)mm × 2.0(±0.20)mm Value to Record: Actual measurements in mm for L, W, and T

Importance: Back glass dimensions directly impact:

- Fit in framing equipment

- Overall module dimensions and mounting compatibility

- Edge sealing effectiveness

Out-of-spec glass can cause:

- Misalignment in automated equipment

- Mechanical stress during framing

- Risk of glass breakage during production or in the field

- Module size inconsistencies

Troubleshooting:

- If dimensions are out of spec, isolate the affected batch

- Check with glass supplier for dimensional issues

- Adjust handling equipment if necessary

- Monitor for patterns in measurement deviations

### 9.2 No. of Holes/Holes Dimension

Test Frequency: Once per shift Equipment Required: Precision calipers, inspection tools Test Procedure:

- Count the number of holes in the back glass

- Measure each hole diameter

- Verify consistent spacing and positioning

- Check for edge chipping around holes

Acceptance Criteria: 3 holes with dimension 12mm±0.5mm Value to Record: Number of holes and their measurements

Importance: Hole dimensions and count impact:

- Junction box mounting security

- Weather sealing capability

- Module certification compliance

- Cable routing

Improper holes can cause:

- Difficulty in junction box installation

- Potential for water ingress

- Glass stress and potential breakage

- Junction box detachment in the field

Troubleshooting:

- If holes are out of specification, check drilling equipment

- Verify drill bit condition and size

- Check for glass positioning errors during drilling

- Inspect for glass thickness variations affecting drilling

## STAGE 10: MODULE REWORK STATION

### 10.1 Cleaning of Rework Station/Soldering Iron Sponge

Test Frequency: Once per shift Equipment Required: Inspection checklist, cleaning materials Test Procedure:

- Inspect rework station for:

  - Accumulated flux residue

  - Solder debris

  - Dust and contaminants

- Check sponge moisture content

- Verify sponge cleanliness

- Ensure all soldering tools are properly organized

Acceptance Criteria: Rework Station should be Clean/Sponge should be Wet Value to Record: "Clean" or areas requiring attention

Importance: Clean rework stations ensure:

- Contamination-free repairs

- Proper solder joint formation

- Accurate rework results

- Reduced chance of introducing defects

Unclean stations can cause:

- Contaminated solder joints

- Poor adhesion of repairs

- Corrosion at connection points

- Potential for introducing debris into module

Troubleshooting:

- Implement regular cleaning schedule

- Train technicians on proper station maintenance

- Replace sponges regularly

- Use appropriate cleaning agents for flux removal

### 10.2 Soldering Iron Temperature

Test Frequency: Once per shift Equipment Required: Calibrated temperature measurement device Test Procedure:

- Allow soldering iron to reach operating temperature

- Use temperature probe or specialized thermometer to measure tip temperature

- Verify temperature readout matches setting

- Check stability of temperature over time

Acceptance Criteria: 400±30°C Value to Record: Actual temperature in °C

Importance: Correct soldering temperature ensures:

- Proper solder flow and joint formation

- Minimal thermal stress on components

- Complete flux activation

- Reliable electrical connections

Incorrect temperatures can cause:

- Cold solder joints if too low

- Component damage if too high

- Inconsistent joint quality

- Excessive flux burnoff

Troubleshooting:

- Calibrate soldering station

- Check for worn or oxidized tips

- Verify thermocouple function

- Replace soldering equipment if temperature cannot be maintained

### 10.3 Method of Rework

Test Frequency: Once per shift Equipment Required: Work instruction document GSPL/QA/WI/009 Test Procedure:

- Observe rework technician performing repairs

- Compare technique to documented work instructions

- Verify proper tools are being used

- Check soldering material quality and type

- Ensure proper cleaning before and after rework

Acceptance Criteria: As per WI (GSPL/QA/WI/009) Value to Record: Compliance status and deviations

Importance: Proper rework method ensures:

- Consistent repair quality

- Minimal thermal stress on cells

- Reliable electrical connections

- Traceable and repeatable process

Incorrect rework can cause:

- Cell damage from excess heat

- Weak electrical connections

- Visual defects

- Reliability issues in the field

Troubleshooting:

- Retrain technicians on proper procedures

- Update work instructions if better methods are identified

- Verify tools are appropriate for the specific rework needed

- Implement regular audits of rework quality

## STAGE 11: STRING REWORK STATION

### 11.1 Cleaning of Rework Station/Soldering Iron Sponge

Test Frequency: Once per shift Equipment Required: Inspection checklist, cleaning materials Test Procedure:

- Inspect string rework station for:

  - Accumulated flux residue

  - Solder debris

  - String fragments

  - Dust and contaminants

- Check sponge moisture content

- Verify sponge cleanliness

- Ensure all soldering tools are properly organized

Acceptance Criteria: Rework Station should be Clean/Sponge should be Wet Value to Record: "Clean" or areas requiring attention

Importance: Clean string rework stations ensure:

- Contamination-free string repairs

- Proper solder joint formation

- Reduced risk of cell damage

- Clear workspace for precise repairs

Unclean stations can cause:

- Contaminated solder joints

- Poor adhesion of repairs

- Increased risk of cell microcracks

- Potential for introducing debris into module

Troubleshooting:

- Implement regular cleaning schedule

- Train technicians on proper station maintenance

- Replace sponges regularly

- Use appropriate cleaning agents for flux removal

### 11.2 Soldering Iron Temperature

Test Frequency: Once per shift Equipment Required: Calibrated temperature measurement device Test Procedure:

- Allow soldering iron to reach operating temperature

- Use temperature probe or specialized thermometer to measure tip temperature

- Verify temperature readout matches setting

- Check stability of temperature over time

Acceptance Criteria: 400±30°C Value to Record: Actual temperature in °C

Importance: Correct soldering temperature for string repair ensures:

- Proper solder flow without damaging cells

- Minimal thermal stress on delicate cell structures

- Complete flux activation

- Reliable electrical connections

Incorrect temperatures can cause:

- Cold solder joints if too low

- Cell damage if too high

- Microcracks from thermal stress

- Inconsistent repair quality

Troubleshooting:

- Calibrate soldering station

- Check for worn or oxidized tips

- Verify thermocouple function

- Replace soldering equipment if temperature cannot be maintained

## STAGE 12: PRE-LAMINATION EL & VISUAL INSPECTION

### 12.1 EL Inspection

Test Frequency: 5 pieces per shift Equipment Required: EL imaging system, document GSPL/IPQC/QC/001 Test Procedure:

- Place module in EL imaging station

- Connect to power supply with appropriate current

- Capture EL image in darkened environment

- Analyze image for:

  - Microcracks

  - Inactive areas

  - String connection issues

  - Cell defects

- Compare against acceptance criteria document

Acceptance Criteria: EL image should fulfill the EL Acceptance Criteria GSPL/ELV/001 Value to Record: "Pass" or specific defects found with positions

Importance: Pre-lamination EL testing reveals:

- Cell and string defects before encapsulation

- Last opportunity to detect electrical issues before lamination

- Verification of string interconnection quality

- Baseline for post-lamination comparison

Defects at this stage indicate:

- Handling damage during layup

- Soldering issues in interconnections

- Cell quality problems

- Potential module performance issues

Troubleshooting:

- If defects are found, determine if they can be repaired

- Categorize by type and location to identify process issues

- Check handling procedures if cracks are common

- Review stringing process if interconnection issues are prevalent

### 12.2 Visual Inspection

Test Frequency: 5 pieces per shift Equipment Required: Inspection light table, document GSPL/IPQC/QC/001 Test Procedure:

- Place module on inspection surface

- Check for:

  - Foreign particles and contamination

  - Ribbon alignment and quality

  - Cell spacing and alignment

  - Broken or chipped cells

  - Backsheet defects

- Verify visual quality meets standards

Acceptance Criteria: Visual image should fulfill the visual acceptance criteria as per GSPL/PLV/001 Value to Record: "Pass" or specific defects found

Importance: Visual inspection ensures:

- Aesthetic quality before lamination

- Detection of obvious physical defects

- Foreign material prevention in final module

- Overall appearance quality

Issues detected can indicate:

- Poor handling procedures

- Contamination in the production environment

- Issues with component quality

- Process inconsistencies

Troubleshooting:

- Clean module if contamination is found

- Replace components with visual defects

- Check environment for sources of contamination

- Review handling procedures to prevent damage

## STAGE 13: LAMINATOR

### 13.1 Monitoring of Laminator Process Parameter

Test Frequency: Once per shift Equipment Required: Laminator control system, specification document GSPL/TS/001 Test Procedure:

- Access laminator control system

- Record the following parameters:

  - Temperature profile (typically 145-155°C peak)

  - Pressure settings

  - Vacuum levels

  - Cycle time

  - Heating and cooling rates

- Compare with specification document GSPL/TS/001

- Verify parameters match current product requirements

Acceptance Criteria: As per Laminator Specification GSPL/TS/001 Value to Record: Actual parameters vs. specification requirements

Importance: Lamination parameters directly affect:

- EVA curing and adhesion

- Cell encapsulation quality

- Overall module durability

- Optical performance

Incorrect settings can cause:

- Undercured or overcured EVA

- Delamination in the field

- Air bubbles or voids

- Cell damage from excess pressure or temperature

Troubleshooting:

- Reset parameters to specification if deviations are found

- Check temperature sensor calibration

- Verify pressure system function

- Check vacuum pump performance

### 13.2 Cleaning of Diaphragm/Release Sheet

Test Frequency: Once every 24 hours Equipment Required: Inspection checklist, approved cleaning materials Test Procedure:

- Inspect diaphragm and release sheets for:

  - EVA residue

  - Contamination

  - Wear or damage

  - Surface irregularities

- Clean using approved methods and materials

- Verify cleanliness after cleaning

- Check for damage that could affect lamination

Acceptance Criteria: Diaphragm/Release sheet should be clean, No EVA residue is allowed Value to Record: "Clean" or specific issues found

Importance: Clean diaphragms/release sheets ensure:

- Even pressure distribution during lamination

- No transfer of contaminants to modules

- Proper release after lamination

- Consistent lamination quality

Contaminated surfaces can cause:

- Module surface defects

- Sticking and handling damage

- Uneven pressure distribution

- Visual defects in the laminate

Troubleshooting:

- Use proper cleaning agents for EVA residue

- Implement regular replacement schedule

- Check for tears or damage that can't be cleaned

- Verify cleaning procedures are being followed

### 13.3 Peel Test Between EVA/Glass and EVA/Backsheet

Test Frequency: All positions, all laminators to be covered in a month Equipment Required: Peel strength tester, sample preparation equipment Test Procedure:

- Cut test strips from laminated samples

- Prepare for 90° or 180° peel testing

- Measure force required to separate:

  - EVA from glass (E/G)

  - EVA from backsheet (E/B)

- Record peak and average forces

- Observe failure mode (adhesive or cohesive)

Acceptance Criteria: E/G ≥60N/cm, E/B≥60N/cm Value to Record: Actual measured force in N/cm

Importance: Peel strength indicates:

- Lamination quality and EVA curing

- Long-term durability against delamination

- Weather sealing effectiveness

- Overall encapsulation quality

Low peel strength can indicate:

- Undercured EVA

- Contamination during layup

- Improper lamination parameters

- Material incompatibility issues

Troubleshooting:

- If below specification, check lamination temperature profile

- Verify EVA quality and expiration date

- Check for contamination in layup area

- Review material compatibility with suppliers

### 13.4 Gel Content Test

Test Frequency: Once per shift Equipment Required: Gel content testing equipment, extraction apparatus Test Procedure:

- Cut small sample of cured EVA from laminated module

- Measure initial weight

- Extract using appropriate solvent

- Measure remaining weight after extraction

- Calculate gel content percentage

Acceptance Criteria: 75 to 95% Value to Record: Actual gel content percentage

Importance: Gel content indicates:

- Degree of EVA crosslinking and curing

- Expected long-term stability

- Resistance to environmental degradation

- Overall encapsulation quality

Improper gel content indicates:

- Undercured (<75%) - prone to delamination, yellowing

- Overcured (>95%) - potentially brittle, stress on cells

- Process inconsistencies

- Potential long-term reliability issues

Troubleshooting:

- If out of range, check lamination temperature profile

- Verify EVA quality and type

- Check cure time in laminator

- Review cooling rate after peak temperature

## STAGE 14: AUTO EDGE TRIMMING

### 14.1 Trimming Quality

Test Frequency: 5 pieces per shift Equipment Required: Visual inspection tools, measuring equipment Test Procedure:

- Inspect trimmed edges of laminated module for:

  - Completeness of trimming

  - Evenness around perimeter

  - Absence of sharp edges

  - Proper depth of cut

  - No exposed glass edges

- Measure distance from cell edge to trimmed edge

- Check for consistency around module

Acceptance Criteria: Excess layer from the glass edge should be removed, Uneven Trimming not allowed Value to Record: "Pass" or specific defects found

Importance: Edge trimming quality affects:

- Frame fit and sealing

- Weather resistance at edges

- Aesthetic appearance

- Safety (no sharp edges)

Poor trimming can cause:

- Irregular frame fit

- Moisture ingress paths

- Poor edge sealing

- Unprofessional appearance

Troubleshooting:

- Check trimming blade alignment and condition

- Verify module positioning during trimming

- Adjust cutting depth if needed

- Ensure consistent module dimensions before trimming

### 14.2 Trimming Blade Life Cycle

Test Frequency: Once per month Equipment Required: Blade inspection tools, maintenance records Test Procedure:

- Check blade edges for:

  - Dullness or rounding

  - Chipping or breaks

  - Uneven wear patterns

  - Surface finish

- Review blade usage count and history

- Compare against expected lifetime

- Inspect cut quality from current blade

Acceptance Criteria: Worn out not allowed Value to Record: Blade condition and usage count

Importance: Blade condition affects:

- Cut quality and precision

- Energy consumption during cutting

- Potential for module damage

- Process efficiency

Worn blades can cause:

- Ragged or incomplete cuts

- Module edge damage

- Increased processing time

- Inconsistent trimming quality

Troubleshooting:

- Replace blades according to schedule

- Rotate or sharpen if applicable

- Check cutting parameters for worn blades

- Monitor for premature wear indicating other issues

I'll provide detailed explanations for each test in Stages 15-28 of the solar module manufacturing quality control process, similar to what you've outlined for Stage 14.

## STAGE 15: 90° VISUAL INSPECTION

### 15.1 Visual Inspection

Test Frequency: 5 pieces per shift
Equipment Required: Light box, magnification tools, visual inspection template
Test Procedure:

- Place module at 90° angle to light source

- Systematically examine entire module surface for:

  - Bubbles or delamination

  - Cell cracks visible at angle

  - EVA discoloration

  - Foreign particles or inclusions

  - Light reflection inconsistencies

- Document any defects with location

- Compare against acceptance criteria

Acceptance Criteria: As per visual inspection criteria GSPL/PLV/002
Value to Record: "Pass" or specific defects found
Importance: 90° inspection reveals:

- Defects not visible in flat position

- Lamination quality issues

- Internal structural problems

- Cell alignment issues

Poor 90° inspection can miss:

- Incipient delamination

- Minor cell cracks that could propagate

- Interface issues between layers

- Optical defects visible only at certain angles

Troubleshooting:

- Ensure proper lighting conditions

- Train inspectors for consistency

- Compare findings with EL results

- Maintain reference samples of common defects

## STAGE 16: FRAMING

### 16.1 Glue Uniformity & Continuity in Frame Groove

Test Frequency: 1 set per shift
Equipment Required: Inspection light, glue pattern template, measuring tools
Test Procedure:

- Inspect frame groove before assembly for:

  - Cleanliness and preparation

  - Absence of debris

- Monitor glue dispensing pattern

- Check assembled frame for:

  - Continuous glue line

  - Even distribution in groove

  - No gaps or voids

  - Proper adhesion to glass edge

Acceptance Criteria: Should be uniform, Back sealing should be proper
Value to Record: Uniformity status and any defects
Importance: Glue uniformity ensures:

- Weathertight seal

- Mechanical strength of frame bond

- Proper load distribution

- Protection against moisture ingress

Poor glue application can cause:

- Water leakage into module

- Frame detachment under load

- Uneven stress distribution

- Premature failure in field

Troubleshooting:

- Check glue dispensing equipment calibration

- Verify glue viscosity and temperature

- Ensure proper frame alignment during assembly

- Check for blockages in dispensing nozzles

### 16.2 Short Side Glue Weight

Test Frequency: Once per shift
Equipment Required: Precision scale, glue sampling tools
Test Procedure:

- Collect glue sample for short side application

- Weigh sample on calibrated scale

- Compare to specification

- Adjust dispensing parameters if needed

Acceptance Criteria: 55±10 gm
Value to Record: Actual weight in grams
Importance: Proper glue quantity ensures:

- Sufficient bonding strength

- Consistent frame sealing

- Cost efficiency

- Process repeatability

Insufficient glue can cause:

- Weak frame attachment

- Incomplete sealing

- Early failure in field conditions

- Inconsistent quality

Troubleshooting:

- Calibrate dispensing equipment

- Check glue supply pressure

- Verify nozzle condition

- Adjust application parameters

### 16.3 Long Side Glue Weight

Test Frequency: Once per shift
Equipment Required: Precision scale, glue sampling tools
Test Procedure:

- Collect glue sample for long side application

- Weigh sample on calibrated scale

- Compare to specification

- Adjust dispensing parameters if needed

Acceptance Criteria: 120±20 gm
Value to Record: Actual weight in grams
Importance: Proper glue quantity ensures:

- Consistent frame adhesion on longer edges

- Proper load distribution

- Uniform sealing around perimeter

- Process stability

Excessive glue can cause:

- Material waste

- Cleanup issues

- Longer curing time

- Inconsistent appearance

Troubleshooting:

- Check for dispensing system fluctuations

- Verify glue viscosity and temperature

- Ensure proper nozzle size and condition

- Adjust dispensing rate or pressure

### 16.4 Anodizing Thickness

Test Frequency: Once per shift
Equipment Required: Coating thickness meter, calibration standards
Test Procedure:

- Select random frame section

- Clean measurement area

- Use calibrated thickness meter

- Take multiple readings at different locations

- Calculate average thickness

Acceptance Criteria: ≥15 micron
Value to Record: Measured thickness in microns
Importance: Anodizing thickness affects:

- Corrosion resistance

- Surface hardness

- Weather durability

- Aesthetic quality

Insufficient anodizing can cause:

- Premature corrosion

- Poor appearance over time

- Reduced lifetime in harsh environments

- Lower scratch resistance

Troubleshooting:

- Verify anodizing process parameters

- Check supplier certification

- Sample from different frame batches

- Implement corrective action with supplier if needed

## STAGE 17: JUNCTION BOX ASSEMBLY

### 17.1 Junction Box (Connector Appearance & Cable Length)

Test Frequency: Once per shift
Equipment Required: Measuring tape, visual inspection aids, connector test fixtures
Test Procedure:

- Verify junction box positioning on module

- Check connector appearance for:

  - Physical damage

  - Complete assembly

  - Proper color coding

  - Alignment of components

- Measure cable lengths

- Inspect cable insulation condition

Acceptance Criteria: As per Process Card & module drawing
Value to Record: Pass/fail and any deviations
Importance: Junction box quality affects:

- Electrical safety

- Connection reliability

- Installation compatibility

- Weather resistance

Poor junction box assembly can cause:

- Electrical failures

- Water ingress

- Installation difficulties

- Connection reliability issues

Troubleshooting:

- Verify junction box alignment fixtures

- Check cable cutting equipment calibration

- Ensure proper component storage conditions

- Train operators on proper handling techniques

### 17.2 Soldering Iron Temperature

Test Frequency: Once per shift
Equipment Required: Calibrated temperature probe, temperature logger
Test Procedure:

- Allow soldering iron to reach stable temperature

- Measure tip temperature with calibrated probe

- Record actual temperature

- Adjust if outside specification

Acceptance Criteria: 400±50°C
Value to Record: Actual temperature in °C
Importance: Proper soldering temperature ensures:

- Good solder flow and wetting

- Strong electrical connections

- Prevention of component damage

- Consistent soldering quality

Improper temperature can cause:

- Cold solder joints (too low)

- Component damage (too high)

- Inconsistent connection quality

- Reduced reliability

Troubleshooting:

- Check temperature controller calibration

- Verify thermocouple condition

- Replace worn tips

- Adjust temperature settings

### 17.3 Soldering Quality

Test Frequency: Once per shift
Equipment Required: Inspection microscope, soldering quality standards, pull tester
Test Procedure:

- Visually inspect soldered connections for:

  - Complete wetting

  - Proper fillet formation

  - Absence of cold joints

  - No excess solder

- Test mechanical strength if needed

- Document any defects

Acceptance Criteria: Welding area should be fully covered & checked by twizzer, no yellowing allowed
Value to Record: Pass/fail with specific observations
Importance: Soldering quality affects:

- Electrical conductivity

- Mechanical strength

- Long-term reliability

- Heat dissipation

Poor soldering can cause:

- Intermittent connections

- High resistance points

- Mechanical failures

- Heat damage

Troubleshooting:

- Check soldering iron tip condition

- Verify flux quality and quantity

- Ensure proper cleaning before soldering

- Train operators on proper technique

## STAGE 18: JB POTTING

### 18.1 A/B Glue Ratio

Test Frequency: Once per shift
Equipment Required: Precision scale, mixing ratio verification tools
Test Procedure:

- Collect samples of A and B components

- Weigh individually on calibrated scale

- Calculate ratio

- Verify against specification

Acceptance Criteria: 5±0.5:1
Value to Record: Actual ratio measured
Importance: Proper mixing ratio ensures:

- Complete curing

- Correct mechanical properties

- Proper adhesion

- Consistent electrical insulation

Improper ratio can cause:

- Incomplete curing

- Soft or brittle potting

- Poor adhesion

- Moisture penetration

Troubleshooting:

- Calibrate dispensing equipment

- Check component viscosities

- Verify pump operation

- Perform regular maintenance on mixing equipment

### 18.2 Potting Material Weight

Test Frequency: Once per shift
Equipment Required: Precision scale, sampling tools
Test Procedure:

- Collect potting material sample

- Weigh on calibrated scale

- Compare to specification

- Adjust dispensing if needed

Acceptance Criteria: 20±3 gm
Value to Record: Actual weight in grams
Importance: Proper potting quantity ensures:

- Complete component encapsulation

- Adequate electrical insulation

- Proper thermal management

- Cost efficiency

Insufficient potting can cause:

- Exposed electrical components

- Inadequate protection

- Air voids and moisture traps

- Premature failure

Troubleshooting:

- Calibrate dispensing equipment

- Check material viscosity

- Verify dispensing pressure

- Adjust dispensing time or rate

### 18.3 Nozzle Changing

Test Frequency: Once every 6 hours
Equipment Required: Nozzle replacement tools, inspection aids
Test Procedure:

- Check current nozzle condition

- Document usage time

- Replace according to schedule

- Verify new nozzle condition

- Validate dispensing pattern after change

Acceptance Criteria: Should be changed after 6 hours or when found issue of damage or extra amount dispensing
Value to Record: Time of change, condition at change
Importance: Regular nozzle changes ensure:

- Consistent dispensing pattern

- Proper material flow

- Prevention of clogging issues

- Process stability

Worn or clogged nozzles can cause:

- Uneven potting distribution

- Inaccurate dispensing amounts

- Material waste

- Quality inconsistencies

Troubleshooting:

- Implement strict nozzle change schedule

- Train operators on proper replacement technique

- Monitor dispensing quality after changes

- Optimize cleaning procedures between uses

### 18.4 Silicon Glue Weight on the Bottom

Test Frequency: Once per shift
Equipment Required: Precision scale, sampling tools
Test Procedure:

- Collect silicon glue sample for bottom application

- Weigh on calibrated scale

- Compare to specification

- Adjust dispensing parameters if needed

Acceptance Criteria: 18±3 gm
Value to Record: Actual weight in grams
Importance: Bottom sealing ensures:

- Complete junction box sealing

- Protection against moisture ingress

- Proper adhesion to backsheet

- Reliable environmental protection

Insufficient bottom sealing can cause:

- Water penetration paths

- Junction box detachment

- Electrical insulation failure

- Reliability issues in field

Troubleshooting:

- Calibrate dispensing equipment

- Check silicon material viscosity

- Verify dispensing pressure

- Adjust application parameters

## STAGE 19: CURING

### 19.1 Temperature

Test Frequency: Once per shift
Equipment Required: Calibrated temperature sensors, data logger
Test Procedure:

- Monitor curing chamber temperature

- Record at specified intervals

- Verify stability within range

- Document any deviations

Acceptance Criteria: 25±3°C
Value to Record: Actual temperature in °C
Importance: Curing temperature affects:

- Potting material cure rate

- Final mechanical properties

- Adhesion quality

- Long-term stability

Improper temperature can cause:

- Incomplete curing

- Material property variations

- Extended curing times

- Inconsistent quality

Troubleshooting:

- Calibrate temperature controllers

- Check heating/cooling systems

- Verify airflow distribution

- Monitor temperature uniformity

### 19.2 Humidity

Test Frequency: Once per shift
Equipment Required: Calibrated humidity sensors, environmental monitor
Test Procedure:

- Monitor curing chamber humidity

- Record at specified intervals

- Verify stability within range

- Document any deviations

Acceptance Criteria: ≥50%
Value to Record: Actual humidity percentage
Importance: Curing humidity affects:

- Cure rate of certain materials

- Prevention of premature drying

- Final material properties

- Process consistency

Improper humidity can cause:

- Surface defects

- Inconsistent curing

- Material property variations

- Quality issues

Troubleshooting:

- Calibrate humidity sensors

- Check humidification system

- Verify chamber sealing

- Adjust humidity control parameters

### 19.3 Curing Time

Test Frequency: Once per shift
Equipment Required: Timer, process monitoring system
Test Procedure:

- Record module entry time

- Monitor total curing duration

- Verify against specification

- Document actual curing time

Acceptance Criteria: ≥4 hours
Value to Record: Actual curing time in hours
Importance: Proper curing time ensures:

- Complete polymerization

- Optimal mechanical properties

- Full adhesion development

- Long-term reliability

Insufficient curing time can cause:

- Incomplete curing

- Reduced mechanical strength

- Poor adhesion

- Premature field failures

Troubleshooting:

- Verify timer accuracy

- Check process flow timing

- Adjust production scheduling

- Implement backup timing systems

## STAGE 20: BUFFING

### 20.1 Corner Edge, Buffing Belt Condition

Test Frequency: 5 pieces per shift
Equipment Required: Magnification tools, edge inspection gauge, belt wear indicators
Test Procedure:

- Inspect module corners for:

  - Smoothness

  - Uniform radius

  - Absence of sharp edges

  - Consistent appearance

- Check buffing belt for:

  - Wear patterns

  - Grit condition

  - Tension

  - Surface integrity

Acceptance Criteria: Should not be sharp & No worn out
Value to Record: Corner condition and belt status
Importance: Proper buffing ensures:

- Safe handling edges

- Reduced stress concentrations

- Uniform appearance

- Prevention of edge damage

Poor buffing can cause:

- Sharp edges creating safety hazards

- Stress points leading to glass breakage

- Unprofessional appearance

- Handling injuries

Troubleshooting:

- Replace buffing belts according to schedule

- Adjust buffing pressure and speed

- Verify belt tracking and tension

- Train operators on proper technique

## STAGE 21: CLEANING

### 21.1 Module Cleanliness

Test Frequency: 5 pieces per shift
Equipment Required: Inspection light, magnification tools, cleaning verification aids
Test Procedure:

- Inspect entire module for:

  - Tape residue

  - Dust and dirt

  - EVA/Backsheet residue

  - Corner burrs

  - Glue residue on glass, backsheet, JB, wire

- Check under angled light for subtle residues

- Document any cleaning deficiencies

Acceptance Criteria: As per visual inspection criteria GSPL/PLV/002
Value to Record: Pass/fail and specific issues
Importance: Proper cleaning ensures:

- Professional appearance

- Customer satisfaction

- Accurate final testing

- Prevention of field contamination

Poor cleaning can cause:

- Customer rejection based on appearance

- Reduced light transmission

- Inaccurate power testing

- Lower perceived quality

Troubleshooting:

- Verify cleaning equipment function

- Check cleaning solution composition

- Optimize cleaning process parameters

- Train operators on inspection techniques

## STAGE 22: FLASH TESTER

### 22.1 Ambient Temperature

Test Frequency: Once per shift
Equipment Required: Calibrated temperature sensor, environmental monitor
Test Procedure:

- Measure ambient temperature in test area

- Record value

- Verify within specification

- Adjust testing parameters if needed

Acceptance Criteria: 25±2°C
Value to Record: Actual temperature in °C
Importance: Ambient temperature affects:

- Test accuracy and repeatability

- Reference cell performance

- Temperature corrections

- Standardized test conditions

Improper ambient temperature can cause:

- Measurement errors

- Inconsistent power ratings

- Customer disputes

- Certification issues

Troubleshooting:

- Monitor HVAC performance

- Control room access during testing

- Schedule testing during stable periods

- Implement temperature monitoring system

### 22.2 Module Temperature

Test Frequency: Once per shift
Equipment Required: Calibrated IR thermometer, temperature sensors
Test Procedure:

- Measure module temperature before testing

- Verify stabilization time

- Record actual temperature

- Apply temperature corrections if needed

Acceptance Criteria: 25±3°C
Value to Record: Actual temperature in °C
Importance: Module temperature ensures:

- Standardized test conditions

- Accurate power measurements

- Reproducible results

- Compliance with standards

Improper module temperature can cause:

- Power measurement errors

- Inconsistent binning

- Warranty issues

- Non-compliance with standards

Troubleshooting:

- Verify module stabilization time

- Check temperature measurement equipment

- Control testing environment

- Apply proper temperature coefficients

### 22.3 Sunsimulator Calibration

Test Frequency: Once per 24 hours
Equipment Required: Reference modules, calibrated reference cell, measurement system
Test Procedure:

- Verify reference cell calibration

- Measure reference module under simulator

- Compare to standard values

- Adjust simulator settings if needed

- Document calibration results

Acceptance Criteria: Sunsimulator must be calibrated at the start of the shift with Golden/Silver module (GSPL/QA/S/11)
Value to Record: Calibration values and adjustments
Importance: Regular calibration ensures:

- Accurate irradiance levels

- Consistent spectral distribution

- Repeatable measurements

- Standard compliance

Poor calibration can cause:

- Systematic measurement errors

- Incorrect module binning

- Customer warranty issues

- Regulatory non-compliance

Troubleshooting:

- Check reference module condition

- Verify measurement system accuracy

- Monitor lamp aging

- Follow prescribed calibration procedure

### 22.4 Validation

Test Frequency: Once every 6 hours
Equipment Required: Reference modules, measurement system, validation records
Test Procedure:

- Measure reference module under standard conditions

- Compare to known values

- Verify system stability

- Document validation results

Acceptance Criteria: As per GSPL/QA/S/11
Value to Record: Validation results and deviation
Importance: Regular validation ensures:

- Measurement system stability

- Early detection of drift

- Process control

- Quality assurance

Poor validation can cause:

- Undetected measurement errors

- Gradual system drift

- Inconsistent product classification

- Customer complaints

Troubleshooting:

- Check reference module condition

- Verify measurement system connections

- Monitor environmental conditions

- Implement regular validation schedule

### 22.5 Silver Reference Module EL Check

Test Frequency: Once every two weeks
Equipment Required: EL imaging system, reference images, analysis software
Test Procedure:

- Capture EL image of silver reference module

- Compare to original reference image

- Check for any changes or degradation

- Document comparison results

Acceptance Criteria: Should be same as original EL picture
Value to Record: Comparison results and any deviations
Importance: Reference module stability ensures:

- Consistent measurement baseline

- System accuracy verification

- Long-term measurement traceability

- Reliable power rating

Reference module changes can indicate:

- Measurement system drift

- Reference module degradation

- Handling damage

- Need for new reference standards

Troubleshooting:

- Properly store reference modules

- Limit handling of reference modules

- Maintain controlled environment for storage

- Establish regular replacement schedule

## STAGE 23: HIPOT TEST

### 23.1 DCW

Test Frequency: 5 pieces per shift
Equipment Required: Calibrated hipot tester, test fixtures, safety equipment
Test Procedure:

- Connect module to hipot tester

- Apply test voltage according to specification

- Measure leakage current

- Record results

- Verify pass/fail status

Acceptance Criteria: ≤50μA
Value to Record: Actual leakage current in μA
Importance: DCW test ensures:

- Electrical safety

- Adequate insulation

- Protection against electric shock

- Compliance with safety standards

Excessive leakage current indicates:

- Insulation defects

- Moisture ingress

- Manufacturing defects

- Safety hazards

Troubleshooting:

- Verify test equipment calibration

- Check test connections and fixtures

- Ensure module is dry and clean

- Investigate failed modules for root cause

### 23.2 IR

Test Frequency: 5 pieces per shift
Equipment Required: Calibrated insulation resistance tester, test fixtures
Test Procedure:

- Connect module to tester

- Apply test voltage

- Measure insulation resistance

- Record results

- Verify pass/fail status

Acceptance Criteria: >40MΩ.m²
Value to Record: Actual resistance in MΩ.m²
Importance: IR testing ensures:

- Adequate electrical isolation

- Long-term reliability

- Prevention of current leakage paths

- Safety compliance

Low insulation resistance indicates:

- Moisture penetration

- Material defects

- Manufacturing errors

- Potential safety issues

Troubleshooting:

- Check test equipment calibration

- Verify test conditions (temperature/humidity)

- Ensure proper module preparation

- Analyze failed modules for defect patterns

### 23.3 Ground Continuity

Test Frequency: 5 pieces per shift
Equipment Required: Calibrated continuity tester, test probes
Test Procedure:

- Connect tester to module frame and ground point

- Measure resistance

- Verify within specification

- Document results

Acceptance Criteria: (0-100) mΩ
Value to Record: Actual resistance in mΩ
Importance: Ground continuity ensures:

- Proper grounding for safety

- Protection against electrical faults

- Compliance with electrical codes

- Personnel safety

Poor ground continuity can cause:

- Electric shock hazards

- Installation compliance issues

- System safety problems

- Potential fire risks

Troubleshooting:

- Check frame anodizing at ground points

- Verify test probe contact

- Ensure clean contact surfaces

- Investigate manufacturing variations

### 23.4 Verification of Process Parameter

Test Frequency: Once per shift
Equipment Required: Process verification checklist, test equipment records
Test Procedure:

- Verify test equipment settings

- Check test sequence and protocols

- Confirm test limits and thresholds

- Document verification results

Acceptance Criteria: As per GSPL/QA/S/12
Value to Record: Verification status
Importance: Process verification ensures:

- Consistent test application

- Proper test equipment configuration

- Test sequence compliance

- Quality assurance

Improper testing parameters can cause:

- Inaccurate test results

- False passes or failures

- Inconsistent quality control

- Potential field reliability issues

Troubleshooting:

- Implement standard test configurations

- Verify equipment calibration status

- Train operators on proper procedures

- Document all test parameters

### 23.5 Voltage & Current Verification in DC Power Supply

Test Frequency: Once per shift
Equipment Required: Calibrated multimeter, power supply verification procedures
Test Procedure:

- Measure actual output voltage of DC power supply

- Verify current limiting function

- Compare to set points

- Document verification results

Acceptance Criteria: As per GSPL/QA/S/12
Value to Record: Actual voltage and current values
Importance: Power supply verification ensures:

- Accurate test conditions

- Reliable test results

- Equipment safety

- Process stability

Incorrect power supply settings can cause:

- Invalid test results

- Equipment damage

- Module damage during testing

- Inconsistent quality control

Troubleshooting:

- Regularly calibrate power supplies

- Implement verification procedures

- Document actual vs. set values

- Train operators on proper verification

## STAGE 24: POST EL TEST

### 24.1 EL Inspection

Test Frequency: 5 pieces per shift
Equipment Required: EL imaging system, reference images, analysis software
Test Procedure:

- Place module in EL imaging chamber

- Capture EL image under controlled conditions

- Analyze for:

  - Cell cracks

  - Inactive areas

  - Connection issues

  - Manufacturing defects

- Compare against acceptance criteria

Acceptance Criteria: EL image should fulfill the EL Acceptance Criteria GSPL/ELV/002
Value to Record: Pass/fail and specific defects
Importance: Post-process EL ensures:

- Detection of handling damage

- Verification of electrical integrity

- Identification of hidden defects

- Final quality control

EL inspection can detect:

- Microcracks from handling

- Broken interconnections

- Inactive cell areas

- Process-induced defects

Troubleshooting:

- Maintain consistent imaging parameters

- Calibrate imaging system regularly

- Train analysts on defect recognition

- Compare with pre-process EL images

### 24.2 Visual Inspection

Test Frequency: 5 pieces per shift
Equipment Required: Light box, inspection template, magnification tools
Test Procedure:

- Inspect module under controlled lighting

- Check systematically for:

  - Surface defects

  - Frame issues

  - Junction box integrity

  - Label placement

  - Overall appearance

- Document any defects found

Acceptance Criteria: Visual image should fulfill the visual acceptance criteria as per GSPL/PLV/002
Value to Record: Pass/fail and specific defects
Importance: Final visual inspection ensures:

- Aesthetic quality

- Detection of handling damage

- Customer acceptance

- Brand quality assurance

Visual inspection catches:

- Cosmetic defects

- Assembly issues

- Labeling errors

- Transportation damage

Troubleshooting:

- Standardize inspection conditions

- Train inspectors on criteria

- Maintain reference samples

- Implement systematic inspection pattern

## STAGE 25: RFID

### 25.1 RFID Position

Test Frequency: Once per shift
Equipment Required: RFID reader, position verification tool
Test Procedure:

- Check RFID tag placement on module

- Verify alignment with designated position

- Test readability from specified distance

- Document position compliance

Acceptance Criteria: As per Process card
Value to Record: Position status and readability
Importance: Proper RFID positioning ensures:

- Consistent tag reading

- Automated inventory tracking

- Installation verification

- Warranty tracking

Improper positioning can cause:

- Failed tag reads

- Tracking system errors

- Difficult field identification

- Customer service issues

Troubleshooting:

- Check positioning fixtures

- Verify tag application process

- Test read reliability

- Train operators on proper placement

### 25.2 Cell & Module Make & Manufacturing Month Verification

Test Frequency: Once per shift
Equipment Required: RFID reader, database verification system
Test Procedure:

- Read RFID tag data

- Verify cell manufacturer information

- Check module manufacturing date

- Confirm data matches actual module

Acceptance Criteria: As per Process card
Value to Record: Data verification status
Importance: Accurate data ensures:

- Product traceability

- Warranty validation

- Quality control tracking

- Material batch identification

Incorrect data can cause:

- Traceability issues

- Warranty disputes

- Inventory management problems

- Customer satisfaction issues

Troubleshooting:

- Verify data input process

- Check RFID programming equipment

- Implement data verification procedures

- Train operators on data verification

## STAGE 26: FINAL VISUAL INSPECTION

### 26.1 Visual Inspection

Test Frequency: 5 pieces per shift
Equipment Required: Inspection light box, visual standards, magnification tools
Test Procedure:

- Perform comprehensive visual inspection:

  - Front glass surface

  - Frame condition and fit

  - Junction box installation

  - Cable and connector quality

  - Label placement and condition

  - Backsheet appearance

- Document any defects

Acceptance Criteria: As per visual inspection criteria GSPL/PLV/002
Value to Record: Pass/fail and specific defects
Importance: Final inspection ensures:

- Overall product quality

- Customer satisfaction

- Brand reputation

- Prevention of defective shipments

Final inspection catches:

- Accumulated handling damage

- Assembly issues

- Labeling errors

- Appearance defects

Troubleshooting:

- Implement comprehensive inspection checklist

- Train inspectors on quality standards

- Maintain reference samples

- Review previous inspection points if issues found

### 26.2 Backlabel

Test Frequency: 5 pieces per shift
Equipment Required: Barcode scanner, label inspection tools
Test Procedure:

- Inspect label for:

  - Print quality and legibility

  - Barcode scan ability

  - Alignment and placement

  - Information accuracy

  - Adhesion quality

- Test barcode scanning

- Verify information matches module

Acceptance Criteria: Air bubble, Tilt, Misprint, folded label not acceptable
Value to Record: Label condition and data verification
Importance: Label quality ensures:

- Product identification

- Installation guidance

- Warranty information

- Regulatory compliance

Label defects can cause:

- Product identification issues

- Warranty validation problems

- Installation difficulties

- Regulatory non-compliance

Troubleshooting:

- Check label printer settings

- Verify label material quality

- Ensure proper application technique

- Train operators on inspection criteria

## STAGE 27: DIMENSION MEASUREMENT

### 27.1 L*W and Module Profile

Test Frequency: Once per shift
Equipment Required: Calibrated measuring tools, dimension verification jig
Test Procedure:

- Measure module length and width

- Check profile dimensions

- Compare to specifications

- Document actual dimensions

Acceptance Criteria: As per Module drawing (±1mm)
Value to Record: Actual dimensions
Importance: Dimensional accuracy ensures:

- Installation compatibility

- Mounting system fit

- Array planning accuracy

- Customer satisfaction

Dimensional issues can cause:

- Installation problems

- Mounting system incompatibility

- Array spacing issues

- Customer returns

Troubleshooting:

- Calibrate measuring equipment

- Check framing equipment setup

- Verify glass cutting dimensions

- Monitor for consistency within batch

### 27.2 Mounting Hole X & Y Pitch

Test Frequency: Once per shift
Equipment Required: Calibrated measuring tools, hole position gauge
Test Procedure:

- Measure distance between mounting holes

- Check X and Y pitch dimensions

- Verify against drawing specifications

- Document actual measurements

Acceptance Criteria: As per Module drawing GSPL/N144/G/001
Value to Record: Actual X and Y pitch dimensions
Importance: Mounting hole accuracy ensures:

- Proper installation

- Compatibility with mounting systems

- Structural integrity

- Load distribution

Inaccurate mounting holes can cause:

- Installation difficulties

- Mounting system incompatibility

- Uneven load distribution

- Potential mechanical failure

Troubleshooting:

- Check frame drilling fixtures

- Verify hole punch alignment

- Monitor for hole elongation

- Implement regular tooling maintenance

### 27.3 Diagonal Difference

Test Frequency: Once per shift
Equipment Required: Calibrated measuring tape, diagonal measurement jig
Test Procedure:

- Measure both diagonals of module

- Calculate difference between measurements

- Compare to specification

- Document results

Acceptance Criteria: ≤3mm
Value to Record: Actual diagonal difference
Importance: Square geometry ensures:

- Proper fit in mounting systems

- Aesthetic appearance in arrays

- Even load distribution

- Professional installation appearance

Continuing with the detailed explanations for the remaining tests:

### 27.3 Diagonal Difference (continued)

Excessive diagonal difference can cause:

- Misalignment in arrays

- Installation difficulties

- Uneven frame stress

- Unprofessional appearance

Troubleshooting:

- Check frame assembly fixtures

- Verify frame component squareness

- Monitor assembly process consistency

- Inspect for frame warping during curing

### 27.4 Corner Gap

Test Frequency: Once per shift
Equipment Required: Feeler gauge, corner inspection tools
Test Procedure:

- Inspect all four corners

- Check for gaps between frame pieces

- Measure any gaps found

- Compare to specifications

Acceptance Criteria: As per Process card
Value to Record: Gap measurements at each corner
Importance: Proper corner sealing ensures:

- Weather resistance

- Structural integrity

- Professional appearance

- Prevention of water ingress

Excessive corner gaps can cause:

- Water penetration

- Frame corrosion

- Reduced structural integrity

- Quality perception issues

Troubleshooting:

- Check corner cutting precision

- Verify frame alignment during assembly

- Ensure proper corner pressure during curing

- Check for frame material variations

### 27.5 JB Cable Length

Test Frequency: Once per shift
Equipment Required: Calibrated measuring tape
Test Procedure:

- Measure cable length from junction box

- Verify against specification

- Check cable routing

- Document actual measurements

Acceptance Criteria: As per Process card
Value to Record: Actual cable lengths
Importance: Correct cable length ensures:

- Installation flexibility

- Array connection compatibility

- Prevention of strain on connections

- Customer satisfaction

Incorrect cable length can cause:

- Installation difficulties

- Connection strain

- Limited configuration options

- Customer complaints

Troubleshooting:

- Verify cable cutting equipment calibration

- Check cable routing guides

- Implement cable length verification fixtures

- Train operators on proper measurement technique

## STAGE 28: PACKAGING

### 28.1 Packaging Label

Test Frequency: Once per shift
Equipment Required: Label verification checklist, barcode scanner
Test Procedure:

- Inspect packaging labels for:

  - Print quality and legibility

  - Information accuracy

  - Barcode scanability

  - Attachment security

- Verify information matches contents

- Document verification results

Acceptance Criteria: As per GSPL/D/SOPP/001
Value to Record: Label compliance status
Importance: Proper labeling ensures:

- Product identification during shipping

- Inventory management

- Customer delivery verification

- Regulatory compliance

Poor labeling can cause:

- Shipping errors

- Inventory confusion

- Regulatory issues

- Customer dissatisfaction

Troubleshooting:

- Verify label printer settings

- Check label material quality

- Ensure proper application method

- Implement verification procedures

### 28.2 Content in Box

Test Frequency: Once per shift
Equipment Required: Packing list, content verification checklist
Test Procedure:

- Verify all required items are included:

  - Module(s)

  - Documentation

  - Accessories (if applicable)

  - Warranty information

- Check quantity against packing list

- Document verification results

Acceptance Criteria: As per BOM and Process card
Value to Record: Content verification status
Importance: Complete packaging ensures:

- Customer satisfaction

- Installation readiness

- Prevention of missing parts claims

- Reduced customer service issues

Incomplete packaging can cause:

- Customer complaints

- Installation delays

- Return processing costs

- Brand reputation damage

Troubleshooting:

- Implement packing checklists

- Train packers on requirements

- Conduct random audits

- Verify BOM against packing instructions

### 28.3 Box Condition

Test Frequency: Once per shift
Equipment Required: Visual inspection, box integrity testing tools
Test Procedure:

- Inspect packaging boxes for:

  - Structural integrity

  - Print quality

  - Moisture damage

  - Assembly quality

- Test box closure security

- Verify protective elements

Acceptance Criteria: Damage, dull printing, wet boxes not allowed
Value to Record: Box condition status
Importance: Package quality ensures:

- Product protection during shipping

- Professional presentation

- Brand perception

- Damage prevention

Poor packaging can cause:

- Shipping damage

- Customer perception issues

- Returns and claims

- Increased shipping costs

Troubleshooting:

- Verify box storage conditions

- Check box assembly equipment

- Implement handling procedures

- Train staff on packaging standards

### 28.4 Wooden Pallet Dimension

Test Frequency: Once per shift
Equipment Required: Measuring tape, pallet verification guide
Test Procedure:

- Measure pallet dimensions

- Check structural integrity

- Verify compatibility with modules

- Document actual dimensions

Acceptance Criteria: Should not be less than module dimension
Value to Record: Actual pallet dimensions
Importance: Proper pallet sizing ensures:

- Product protection

- Shipping stability

- Compatibility with handling equipment

- Efficient space utilization

Improper pallet sizing can cause:

- Product overhang and damage risk

- Handling difficulties

- Shipping inefficiencies

- Storage problems

Troubleshooting:

- Verify pallet supplier specifications

- Check for pallet damage or warping

- Ensure proper assembly

- Implement pallet inspection procedures

This comprehensive breakdown of each quality control test in Stages 15-28 provides detailed information about test frequency, equipment, procedures, acceptance criteria, importance, potential issues, and troubleshooting approaches for each quality checkpoint in the solar module manufacturing process. These quality controls ensure that the final product meets all specifications for performance, safety, reliability, and appearance.