# IPQC Check Sheet Explanation

This document is an In-Process Quality Control (IPQC) check sheet for solar panel manufacturing at Gautam Solar Private Limited. It outlines quality control parameters that need to be monitored throughout the production process. Let me walk you through each stage, parameter, and what values need to be filled in.

## Stage 1: Shop Floor Environment

These parameters ensure proper manufacturing conditions:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Temperature | 25±2°C | Manufacturing environment must be maintained at 23-27°C to ensure proper material behavior |
| Humidity | RH ≤60% | Relative humidity must be below 60% to prevent moisture issues during manufacturing |

## Stage 2: Glass Loader

Checks the raw materials for the front glass:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Glass dimension (L×W×T) | 2272(±1.5)×1128(±1.5)×2(±0.20) mm | Verifies glass dimensions are within tolerance |
| Appearance (Visual) | No breaks, cracks, scratches or line marks | Visual inspection to ensure glass integrity |

## Stage 3: EVA/EPE Cutting

Checks for the encapsulant material:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| EVA/EPE Type | As per approved BOM | Verifies correct encapsulant material is being used |
| EVA/EPE dimension (L×W×T) | As per specification | Confirms encapsulant is cut to proper dimensions |
| EVA/EPE Status | No dust, foreign particles, cuts, non-uniform embossing | Checks material quality before use |

## Stage 4: Cell Cutting Machine & Cell Loading

Checks solar cell parameters:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Cell Manufacturer & Efficiency | As per document GSPL/IPQC/QA/001 | Verifies correct cells from approved manufacturer |
| Cell Size (L×W) | As per document GSPL/IPQC/QC/006 | Confirms cell dimensions meet specifications |
| Cell Condition | Refer document GSPL/IPQC/QC/009 | Checks for cell defects prior to assembly |
| Cleanliness of Cell Loading Area | No unwanted materials in loading area | Ensures clean environment for cell placement |

## Stage 5: Tabber & Stringer

Monitors the cell interconnection process:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Verification of Process Parameter | Refer Process Card | Confirms machine settings match specifications |
| Cell Cross Cutting | Both side cutting should be equal | Ensures proper cutting symmetry |
| String Length | Refer document GSPL/PLV/003 | Verifies interconnected string meets length requirements |
| Cell to Cell Gap | Refer document GSPL/ELV/003 | Checks spacing between cells in a string |
| Verification of Soldering | Refer Process Card | Visual check of solder connections |
| Peel Strength | ≥1N | Tests the strength of soldered connections |
| Visual Check after Stringing | Per GSPL/IPQC/QA/001 | Inspection after stringing process |
| EL Image of Strings | Per GSPL/ELV/003 | Electroluminescence testing to detect cell defects |

## Stage 6: Auto String Layup

Checks string layout parameters:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| String to String Gap | Refer Process Card & Module Drawing | Verifies proper spacing between strings |
| Cell edge to Glass edge distance | TOP, Bottom, Sides as per Drawing | Ensures correct placement within module |
| Soldering Peel Strength | ≥4N | Tests strength of string interconnections |
| Terminal busbar to edge of Cell | As per spec GSPL/TS/008 | Verifies busbar placement |
| Soldering Quality | No dry/poor soldering | Visual inspection of solder connections |
| Creepage Distance | As per process card/drawing | Checks electrical isolation distances |

## Stage 7: Auto Bussing & Tapping

Monitors the bussing process:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Verification of Process Parameter | As per machine specification | Confirms automation settings |
| Quality of auto taping | Proper taping, no cell shifting | Ensures cells remain positioned correctly |
| Position of RFID & Logo | Should not be tilted | Verifies correct placement of identification |

## Stage 8: Back Glass Loader

Checks the back glass parameters:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Glass dimension (L×W×T) | 2272(±1.5)×1128(±1.5)×2.0(±0.20)mm | Verifies dimensions are within tolerance |
| No. of Holes/Holes dimension | 3 holes with dimension 12mm±0.5mm | Confirms junction box holes meet spec |

## Stage 9: EVA/EPE Cutting (for back side)

Similar to stage 3, but for back encapsulant:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| EVA/EPE Type | As per specification | Verifies correct encapsulant material |
| EVA/EPE dimension (L×W×T) | 2272(±1.5)×1128(±1.5)×2.0(±0.20)mm | Verifies dimensions |
| EVA/EPE Status | No dust, foreign particles, cuts | Checks material quality |

## Stage 10-11: Rework Stations

For manual repairs and corrections:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Cleaning of station/sponge | Station should be clean, sponge wet | Ensures clean repair environment |
| Soldering Iron Temperature | 400±30°C | Verifies correct soldering temperature |
| Method of Rework | As per Work Instruction | Ensures repairs follow procedures |

## Stage 12: Pre-lamination EL & Visual Inspection

Quality checks before lamination:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| EL Inspection | Per GSPL/ELV/001 | Electroluminescence testing to detect cell defects |
| Visual inspection | Per GSPL/PLV/001 | Visual defect inspection |

## Stage 13: Laminator

Monitors the lamination process:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Laminator Process parameters | Per GSPL/TS/001 | Checks temperature, pressure, time profiles |
| Cleaning of Diaphragm/release sheet | No EVA residue allowed | Ensures clean lamination equipment |
| Peel of Test | E/G ≥60N/cm, E/B≥60N/cm | Tests bond strength between layers |
| Gel Content Test | 75 to 95% | Measures EVA curing completeness |

## Stage 14: Auto Edge Trimming

Checks edge quality after lamination:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Trimming Quality | No excess layer, even trimming | Visual check of edge trimming |
| Trimming Blade life cycle | No worn-out blades allowed | Equipment maintenance check |

## Stage 15: 90° Visual Inspection

Visual check at 90° angle:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Visual Inspection | Per GSPL/PLV/002 | Detection of defects visible at 90° angle |

## Stage 16: Framing

Checks the aluminum frame application:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Glue uniformity & continuity | Uniform, proper back sealing | Ensures frame adhesive is applied evenly |
| Short Side Glue Weight | 55±10 gm | Verifies correct amount of adhesive |
| Long Side Glue Weight | 120±20 gm | Verifies correct amount of adhesive |
| Anodizing Thickness | ≥15 micron | Checks frame coating thickness |

## Stage 17: Junction Box Assembly

Checks junction box installation:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Silicon Glue Weight | 18±3 gm | Verifies correct amount of adhesive |
| Soldering Iron Temperature | 400±50°C | Ensures proper soldering temperature |
| Soldering Quality | Fully covered, no yellowing | Visual check of solder connections |
| JB Appearance & Cable Length | As per process card & drawing | Ensures proper components used |

## Stage 18: JB Potting

Checks the junction box potting process:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| A/B Glue Ratio | 5±0.5:1 | Correct mixing ratio of two-part adhesive |
| Potting material weight | 20±3 gm | Proper amount of potting material |
| Nozzle Changing | Changed after 6 hours or when damaged | Equipment maintenance check |

## Stage 19: Curing

Monitors the adhesive curing process:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Temperature | 25±3°C | Proper curing temperature |
| Humidity | ≥50% | Minimum humidity for proper curing |
| Curing Time | ≥4 hours | Minimum time for complete curing |

## Stage 20-21: Buffing and Cleaning

Final surface preparation:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Corner Edge, Buffing belt condition | Not sharp, no worn out | Equipment check for proper finishing |
| Module cleanliness | Free from tape, dust, residue, burrs | Ensures clean final product |

## Stage 22: Flash Tester

Electrical performance testing:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Ambient Temperature | 25±2°C | Proper testing environment |
| Module Temperature | 25±3°C | Stabilized module temperature |
| Sunsimulator Calibration | Per GSPL/QA/S/11 | Equipment calibration check |
| Validation | Per GSPL/QA/S/11 | Validation of measurements |
| Silver Reference Module | Same as original EL picture | Reference standard check |

## Stage 23: Hipot Test

Electrical safety testing:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| DCW | ≤50μA | Dielectric withstand current limit |
| IR | >40MΩ.m² | Insulation resistance minimum |
| Ground Continuity | (0-100) mΩ | Frame grounding resistance |
| Process Parameter | Per GSPL/QA/S/12 | Verifies test equipment settings |
| Voltage & Current Verification | Once per shift | Equipment calibration check |

## Stage 24: Post EL Test

Final electroluminescence inspection:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| EL Inspection | Per GSPL/ELV/002 | Final EL check for defects |
| Visual inspection | Per GSPL/PLV/002 | Final visual inspection |

## Stage 25-26: Final Visual Inspection

Final product appearance check:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| Visual Inspection | Per GSPL/PLV/002 | Comprehensive visual check |
| Backlabel | No air bubbles, tilt, misprints | Label quality check |

## Stage 27: Dimension Measurement

Final product measurements:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| L×W and Module Profile | Per Module drawing (±1mm) | Overall dimension check |
| Mounting Hole X & Y Pitch | Per Process card | Mounting hole positioning |
| Diagonal Difference | ≤3mm | Module squareness check |
| Corner Gap | Per Process card | Frame corner gap check |
| JB Cable length | Per Process card | Correct cable length |

## Stage 28: RFID & Packaging

Final identification and packaging:

| Parameter | Acceptance Criteria | Explanation |
| --- | --- | --- |
| RFID Position | Per visual inspection criteria | Correct placement of identification |
| Cell & Module Make & Manufacturing Month | Once per shift | Verification of product details |
| Packaging Label | Per GSPL/D/SOPP/001 | Proper labeling of packaging |
| Content in Box | As per BOM and Process card | Correct package contents |
| Box Condition | No damage, dull printing, wet boxes | Package quality check |
| Wooden Pallet dimension | Not less than module dimension | Shipping container size check |

## How to Fill the Check Sheet

For each parameter:

- Record the time of inspection

- Enter the measured value or observation in the "Monitoring Result" column

- Note any deviations in the "Remarks, if any" column

- For samples requiring S.No entries, record the serial numbers of modules checked

- The person performing the inspection should sign under "Checked By"

- A supervisor or quality manager should sign under "Reviewed By"

This comprehensive check sheet ensures that every step of the solar panel manufacturing process is monitored for quality and consistency.